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ERLITE ERGO UNI


Erlite Ergo Uni is a three-layer firefighting suit developed based on the experience and needs of Czech professional firefighters. The suit combines the Austrian know-how of seamTEX, a leading manufacturer of firefighting garments, with the Czech manufacturing tradition of Holík.

It is built on the PREMIUM-N/NXT material system, whose performance is based on a carefully engineered combination of materials and a unique layer construction. The result is a balanced combination of protection, breathability, low weight and ergonomics.
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Color:			Navy Blue
Outer material: 		Nomex® Outershell Tough
Sizes: 			XS–4XL (length options: N, K, KK, L, LL))				
OUTSTANDING PROTECTION
thanks to Nomex® and Kevlar® aramid materials  

HIGH BREATHABILITY
seamTEX® PTFE Fire Insert membrane for effective water vapour transmission and reduced heat stress

LOW WEIGHT
ultra-lightweight material construction with a total weight of up to 500 g/m²

ERGONOMICS
pre-shaped knees with foam padding for comfortable movement when kneeling


SeamTEX PREMIUM-N/NXT Material System Outershell Tough designed for demanding firefighting operations and extreme emergency response conditions.

· Material composition: 75% Nomex®, 23% Kevlar®, 2% antistatic fibre
· High mechanical resistance while maintaining low weight
· Hydrophobic treatment resistant to up to 30 washing cycles without re-impregnation

THERMAL INSULATION AND LINING
· Combination of aramid fleece and FR viscose with aramid fibres for thermal comfort and effective moisture management.

MEMBRANE
· Extremely lightweight PTFE membrane with a weight of 90 g/m² ensures high breathability with minimal weight.
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STANDARDS:
ISO 13506-2
EN 469 Xf 2, Xr 2, Y 2, Z 2
EN 1149-5
EN 343 Class 4/4
EN ISO 11612 A1, B2, C1, F2
 






Arclin®, the Arclin logo, Kevlar®, Nomex®, Firepoint® and all trademarks and service marks denoted with ™, SM or ® are owned by Arclin and its affiliates unless otherwise noted. © 2026 Arclin. All rights reserved.
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CARE AND WASHING:
Select a gentle 60 °C wash programme with pre-wash. Use detergent for coloured or delicate laundry. Do not use fabric softener, bleach or organic solvents. Spin at a maximum of 800 rpm and tumble dry gently at low temperature only.
For more about washing and maintenance, see the QR code or visit:
www.holik.com > Technologies > Care & Maintenance
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